LIQUEFIED PETROLEUM GAS (LPG)

Specifications required for the LIQUEPIED PETROLEUM GAS 50%Propane/50%Butane mixed

| PROPERTY | UNITS | TEST METHOD | VALUE |
| --- | --- | --- | --- |
| Ethane | mol % | G.C | 0.08 max. |
| Propane | mol % | G.C | 2 max. |
| Total - C4 | mol % | G.C | 97.5 min. |
| Total – C5 | mol % | G.C | 0.82 max. |
| Sp.Gr.@ (60oF/ 60oF) | --- | ASTM D-2598 | To Be Reported |
| Copper Corrosion | --- | ASTM D-1838 | No. 1a max. |
| Total Sulphide | wt.ppm | (Based On ASTM D-3246) | 30 max. |
| Hydrogen Sulphide | vol.ppm | ASTM D-2420 / DRAGER | Nil |
| Vapor Press@(100 oF) | Psig | ASTM D-2598 | 70 max. |
| Water Content | vol.ppm | Shaw Dew Point | 10 max. |
| Residue on Evaporation | vol % | ASTM D-2158 | 0.05 max |

SPECIFICATION (Propane)

| PROPERTY | UNITS | TEST METHOD | VALUE |
| --- | --- | --- | --- |
| Ethane | mol % | G.C | 0.4 max. |
| Propane | mol % | G.C | 98 min. |
| Butane | mol % | G.C | 1.4 max. |
| Pentanes & Heavier | mol % | G.C | 0.01 max. |
| Copper Corrosion | --- | ASTM D-1838 | No. 1a max. |
| Hydrogen Sulphide | vol.ppm | ASTM D-2420 / DRAGER | 5 max. |
| Sp.Gr.@ (60oF/ 60oF) | --- | ASTM D-2598 | To Be Reported |
| Sulphur (Volatile) | wt.ppm | (Based On ASTM D-3246) | 30 max. |
| Vapor Pressure@(100 oF) | Psig | ASTM D-2598 | 200 max. |
| Water Content | --- | ASTM D-2713 | pass |

|  | LPG |
| --- | --- |
| GENERAL |  |
| > Conforming to Indian Standard specifications | IS 4576 / IS 14861 |
| > Vapor Pressure at 65 oC (Max) Kg/cm2 | 16.87 |
| > Volatility. Evaporation temp. in oC For 95% volume at NTP | 2 |
| > Copper strip corrosion at 38 oC | Not Worse Than 1 |
| > Dryness | No free entrained water |
| > Odour | Level 2 |
| CHEMICAL COMPOSITION |  |
| Ethane % | 1 max |
| Propane % | 38 max |
| Is-Butane % | 19 max |
| Nor-Butane % | 41 min |
| Iso-Pentane and olefins % | 1 max |
| Volatile sulfur % | 0.003 max |
| LIQUID |  |
| Density at 15 oC Kg/liter | 0.557 |
| Volume of liquid per kg at 15 oC Liters | 1.85 |
| Vapor pressure at 15 oC Bar | 5.3 |
| Gross Calorific Value Kcal/kg | 11840 |
| Net Calorific Value Kcal/kg | 10920 |
| Boiling Point at atmospheric pressure oC | 0 |
| VAPOR |  |
| Density at 15 oC Kg/m3 | 2.21 |
| Volume of gas per kg at 15 oC m3 | 0.48 |
| Latent heat of vaporization at 15 oC Kcal/kg | 86 |
| Gross Calorific Value Kcal/Nm3 | 26200 |
| Net Calorific Value Kcal/Nm3 | 24100 |
| Air required for combustion m3/m3 | 29 |